## Slide 1
Samsung SSD 850 PRO 128GB
Cost Analyze
2014/Aug/12
LiteON IT/SSD BU/NVM Central Lab

## Slide 2: Summary
Product under analysis
  Samsung SSD 850 PRO 128GB
Report coverage
  BOM analysis
  FLASH decap analysis
  3D V-NAND TEM analysis
    Line1 for Bit line direction
    Line2 for Word line direction
  Estimated cell layout

## Slide 3: Samsung SSD 850 PRO 128GB-BOM
Bill of Material - Component Count |  |  |  | 
 | Count | MFG | Part # | Package
FLASH 3D V-NAND MLC, DDP | 2 | Samsung | K9LPGY8S1M | 316-FBGA
FLASH 3D V-NAND MLC, QDP | 2 | Samsung | K9HQGY8S5M | 316-FBGA
MDX controller 3-core ARM-Cortex-R4 supports SATA 6Gb/s | 1 | Samsung | S4LN045X01-8030 | FBGA
DRAM: LPDDR 2Gb, 1CHx32 | 1 | Samsung | K4P2G324ED-FGC2 | 168-FBGA, 12x12
SATA Interface Connector | 1 | Unknow | Unknow | std
Power Management IC for SSD | 1 | NA | AOM4HZ | 32-VQFN 5x5
LOAD SWITCH | 1 | TI | TPS22966 (RB966) | 14-SON
power supervisor / charge pump? | 1 | NA | 2BO ACW 4ZB | SOIC 8pin
Unknow IC | 1 | NA | JS4IAD | 10-SON
Unknow IC | 1 | NA | HMR | SOT25
Crystal | 1 | NA | L.T | NA
Capacitor(0402) | 51 | NA | NA | 0402
Capacitor(0603) | 25 | NA | NA | 0603
Capacitor(0805) | 2 | NA | NA | 0805
Resistor(0402) | 41 | NA | NA | 0402
Diode | 2 | NA | NA | 0402
BAED | 6 | NA | NA | 0805
Total component | 140 |  |  | 
53mm
53mm

## Slide 4: 3D V-NAND Decap Analysis
Die Size (mm2) W/O Scribe Line | 12.497*6.739
Die Size (mm2) W/ Scribe Line | 12.567*6.809
Array size (mm2) | 5.922 * 4.262*2
Array Efficiency | 59.94%
Plane/Die | 2
Capacity/Die | 86Gbit
128GB Configuration | DDP*2+QDP*2
Total Die in 128GB | 12 dice
over position | 0.781%
Line 1
Line 2
Line1 & Line2 are TEM cross section sample position

## Slide 5: TEM Cross Section: Line 1
Total 38 layers
  32 wordlines
  4 dummy wordlines
  1 select transistor on top
  1 select transistor on bottom
Feature size:
  Poly pillar diameter:
  106.35nm(top) / 75.2nm(bottom)
  Poly pillar depth / AR: 2894.5nm / 26
  Poly pillar pitch: 239.56 (max)
  Layer thickness: WL/Oxide=30 nm / 28nm = 58nm
以DRAM製程經驗，有潛力可以做到50以上
因為WL平面切得很細(僅隔4根柱子就切開)，所以WL厚度不需要太厚

## Slide 6
因為WL平面切得很細(僅隔4根柱子就切開)，所以WL厚度不需要太厚
鍍鎢金屬時氣體流進word line平面不用跑太遠，所以厚度30nm已足夠
此頁是註解

## Slide 7: TEM Cross Section: Line 2
Shared WL plane
Feature size:
  Poly pillar diameter: 110.08nm (max)
  Poly pillar pitch: 319.08 (max)
  柱狀邊牆 (Channel poly / Tunneling Oxide / Nitride):
  19.79nm / 5.08nm / 5.81nm
Channel Poly
Tunnel Oxide
Charge Trap Nitride
Filling Oxide (單純填充而已)

## Slide 8
BL
Poly Pillar
SL
Line 1
BL
Line 2
110nm
130nm
210nm
Line 2
742.31nm
320nm
Minimum size F=110nm
=4.9 (F2)
Line 1
WL plane

## Slide 9
如果2D是4F2/cell
Array efficiency: 2D: 80%, 3D: 60%, => Ratio: 80%/60%=1.33
則3D的cell密度相當於2D的=24.8 (nm)製程。
則3D的cell密度相當於2D的 F==21.53(nm)製程。
Chart: Layer #
| 32 | 48 | 64 | 96
2D process | 24.8402 | 17.5867 | 15.2305 | 12.4357
Layer # | 2D process
32 | 24.8
48 | 17.6
64 | 15.2
96 | 12.4

## Slide 10: TCAT – Fabrication Process
Line 1
Line 2